## Slide 1: A6: Nanowires grown from photocatalytically active organic nanotubular templates
S. Kirstein / J.P. Rabe

## Slide 2: Proposal for 1st period
 | Year 1 | Year 2 | Year 3 | Year 4
Student 1 | Ag-nanowires: Optimization of wire growth |  | Addition of dye layers | Explore Au, Pt, ZnO…
Student 2 | Nano-manipulation | Local optical spectroscopy |  | IR-spectroscopy
Main objectives:
principles of wire formation
new wire materials
Plasmon modes
Coupling plasmons - dyes

## Slide 3: Approval of 1st period
 | Year 1 | Year 2 | Year 3 | Year 4
Egon Steeg | Ag-nanowires: Optimization of wire growth |  | Addition of dye layers | Explore Au, Pt, ZnO…
 | Nano-manipulation | Local optical spectroscopy |  | IR-spectroscopy

## Slide 4: Approval of 1st period
 | Year 1 | Year 2 | Year 3 | Year 4
Egon Steeg | Ag-nanowires: Optimization of wire growth |  | Addition of dye layers | Explore Au, Pt, ZnO…
 | Nano-manipulation | Local optical spectroscopy |  | IR-spectroscopy
Yan Qiao (post-doc):
RT synthesis in solution of ZnO, ZnS, NiS, CdS at / in aggregates
Addition of CdTe-Qdots to aggregates

## Slide 5: Approval of 1st period
 | Year 1 | Year 2 | Year 3 | Year 4
Egon Steeg | Ag-nanowires: Optimization of wire growth |  | Addition of dye layers | Explore Au, Pt, ZnO…
 | Nano-manipulation | Local optical spectroscopy |  | IR-spectroscopy
Yan Qiao (post-doc):
RT synthesis in solution of ZnO, ZnS, NiS, CdS at / in aggregates
Addition of CdTe-Qdots to aggregates
Katie Herman(Master thesis)
Nano-manipulation of Ag Nanowires byAFM

## Slide 6: Results I: Ag nanowire Growth
Dye + AgNO3
Na+ Cl-
E. Steeg, H. Kirmse, F. Polzer, Y. Qiao, J. P. Rabe, S. Kirstein, in prep.
Site of nuclei: wire or particle
Competitive growth
Ag transport through wall
Oxidative etching of wires
AgCl on cost of Ag
Dynamics on scale of days
Z2 (Kirmse)
Notes: Bessere Bilder!

## Slide 7: Results II: Ag nanowire Structure
SAED of single wires
Additional characterization:
HRTEM  crystalline domains, twin boundaries.
EDX  silver.
Xray-Microscopy (absorption edge)  silver.
E. Steeg, F. Polzer, H. Kirmse, J. P. Rabe, S. Kirstein, in prep.
Z2 (Kirmse)
Crystalline domains
Orientated along wire axis
Ag diffraction pattern
Additional pattern of superstructure or twins.
Z2 (Kirmse)
A9 (Kowarik)
Notes: Aus Egons Vortrag / Auswertefolien

## Slide 8: Results III: Plasmon spectroscopy
Dark field microscopy
Spectroscopy of scattered light
B1 (Kewes / Benson)
5 µm
Wire
Wavelength / nm
300 400 500 600 700
Calculated scattering intensity
Broad plain spectra.
To do:
Lower background (Condensor)
high conc. of wires
L = infty
Notes: Aus Egons Vortrag / Auswertefolien

## Slide 9: Results IV: In-situ Chemistry
Inorganic polycrystalline shell, variable thickness
Various Materials: NiS, ZnS
Strong excitation energy transfer between particle and dyes
Y. Qiao, F. Polzer, H. Kirmse, E. Steeg, S. Kirstein, J. P. Rabe, J. Mater. Chem. C, 2014, Advance Article
Z2 (Kirmse)

## Slide 10: Results V: FRET with Qdots
Y Qiao, F. Polzer, H. Kirmse, E. Steeg, S. Kühn, S. Friede, S. Kirstein, J. P. Rabe, ACS Nano, subm.
Adsorption of commercial CdTe particles, using PDADMAC as glue.

## Slide 11: Results V: FRET with Qdots
Y Qiao, F. Polzer, H. Kirmse, E. Steeg, S. Kühn, S. Friede, S. Kirstein, J. P. Rabe, ACS Nano, subm.
Z2 (Kirmse) B5 (Kühn)
FRET efficiency: type (A): 99% type (B): 50%
(A)
(B)

## Slide 12: A6: HIOS based on nanotubular J-aggregates
(Proposal 2. period)

## Slide 13: Objective: Long range EET
Donor
Acceptor
2R0 = 4..8 nm
2R0
d
Exciton diffusion length LDiff
hv
hv
Ldiff > 2R0 !?
Notes: Hier Konzept des Etransfers „durch das Aggregat“

## Slide 14: Work plan: statistical approach.
Adsorption of Donor / Acceptor particles in various concentration  mean distance L
Characterisation by cryo-TEM  probe of L
Static / time-dependent spectroscopy  efficiency
Exciton diffusion length.
A5(Henneb.)
Z2 (Kowarik)
Charge transfer effects?
Local sructural distortion?
B6 (May)
Notes: Hier Aggregat + polymer + Qdot; verschiedene Qdots; esnsemble Messungen
Collaborations: Z2 (analytics); A5/B3 : time resolved fluorescence ; B6 theory

## Slide 15: Work plan: structure control.
Qdots of different size  commercial (narrow distribution!)
Glue: Polyelectrolyte (+ dye labels  new acceptors!)
SiO2 Coverage  stiffening / isolation / thickness variable
Glue
d
Notes: Hier Aggregat + polymer + Qdot; verschiedene Qdots; esnsemble Messungen
Collaborations: Z2 (analytics); A5/B3 : time resolved fluorescence ; B6 theory

## Slide 16: Work Plan: SiO2 - shell
Y Qiao, F. Polzer, H. Kirmse, S. Kirstein, J. P. Rabe, in prep.
Sol-gel process @ room temp.
No structural distortion
Super-structure!
Notes: Lokale MEssungen

## Slide 17: Objective: SiO2 - shell for structure investigation
Joint project with FU (C. Böttcher):
- cryo-TEM, 3D reconstruction - variation of silica shells - variation of dyes / aggregate structures
J. Megow, et al. in prep.
Super strucure:
periodic
helical
high contrast
 3D reconstruction,
 3D tomography.
?
Correlation
Aggregate structure  SiO2 shell
Notes: Lokale MEssungen