## Slide 1: B7: Charge Transfer and Charge Separation Across Hybrid Interfaces
Ilja Lange, Sina Reiter, Fortunato Piersimoni, Dieter Neher
University of Potsdam
Potsdam-Golm
Understanding of charge injection across a chemically and energetically well-defined hybrid interface
Energetics and split-up of charge transfer excitations at the hybrid interface

## Slide 2: Charge Injection Across the Hybrid Interface
Top Electrode
Substrate
Organic Semiconductor
Bottom Electrode
molecular orientation
density of states
surface profile
work function
chemical composition
doping concentration
energy alignment

## Slide 3: Towards Well-Defined Morphology and Energetics
I. Lange, S. Hecht, S. Kowarek, C. Wöll, G. Heimel, D. Neher et al., AFM online 2014
3 m

## Slide 4: Unipolar Currents Across the Hybrid Interface
I. Lange, et al., AFM online 2014
PCBM LUMO
P3HT HOMO
=> efficient electron and hole injection

## Slide 5: Unipolar Currents Across the Hybrid Interface
I. Lange, et al., AFM online 2014
PCBM LUMO
P3HT HOMO
=> efficient electron and hole injection

## Slide 6: Unipolar Currents Across the Hybrid Interface
Extend approach to other surfaces
Epitaxially Grown ZnO

## Slide 7: Goals and Support
Application of vacuum-processable molecules
Analysis of energetics (interface energetics and band bending)
Work function fine tuning via blends of SAM molecules
Effective medium modeling of charge injection and transport

## Slide 8: Excitations at the Hybrid Type II Heterojunction
Gelinas et al., Science 343, 512 (2014)
should be state with lowest energy

## Slide 9: Charge Generation in Organic Solar Cells
HOT

## Slide 10: Charge Generation in Organic Solar Cells
IQE for organic bulk heterojunction cells is independent of excitation energy over the entire accessible energy range
=> precursor to free charge is always a thermalized CT manifold coupled to CT0
K. Vandewal, S. Albrecht, D. Neher, A. Salleo et al., Nature Materials 13, 63 (2014)
S. Albrecht, K. Vandewal, A. Salleo, D. Neher et al., Adv. Mater. 26 2533 (2014)
COLD

## Slide 11: Delocalisation of Excited States
Tamura and Burghardt, JACS 135, 16364 (2013)
Gelinas et al., Science 343, 512 (2014)
G. Wu et al., J Phys Chem. Lett 4, 2649 (2014)
CT excitons at the polymer:fullerene interface are highly delocalized
but strongly localized at the polymer:ZnO interface

## Slide 12: Hybrid CT Energy Tuning
Combine ZnO with -NPD
deposition from vacuum or solution
suitable HOMO
high bandgap
Koch et al.)

## Slide 13: Planar ZnO-Organic Solar Cells
-NPD

## Slide 14: CT Emission with SAM-functionalized ZnO

## Slide 15: Goals
Tuning of hybrid CT state energy versus COM singlet/triplet enegry
Quantification of efficiency of free charge generation as function of excitation energy
Study of transient properties of all relevant excitations (new fs setup)

## Slide 16: Collaborations
Further improvement of substrate electrode quality (also nanostructured)
Control of ZnO doping (Henneberger)
New SAMs for lowering the ZnO workfunction (Hecht)
New SAMs with covalently attached chromophores (Hecht)
Switchable SAMs (Hecht)
Energetics at the interface and in the organic layer (Koch, Heimel)
Energetics and dynamics of hybrid CT states (Stähler, May, Draxl, Blumstengel etc.)
Coupling of hybrid CT excitons to plasmons (Henneberger)

## Slide 17: Our Aims
Understanding of charge injection across a chemically and energetically well-defined hybrid interface
establish hybrid interfaces as model systems for charge injection
optimization of devices via fine tuning of charge injection and extraction
Energetics and split-up of charge transfer excitations at the hybrid interface
establish hybrid interface as model systems for type II heterojunctions
free charge generation across the interface: hot or cold