## Slide 1: A2 Assembly and local probing of single molecules and defects on ultra-thin ZnO films on metals
Takashi Kumagai, Martin Wolf
Fritz-Haber Institute
Notes: The title of our research project is assembly and local probing of single molecules and defects on ultra-thin ZnO films on metals.

## Slide 2
Basic idea of our project
“Ultrathin ZnO films on metal substrate as model system, study by UHV-LT-STM/AFM”
The relation between geometric and electronic structures (energy level alignment) of organic molecules and defects on ZnO surface at the single atom/molecule level.
STS is powerful to learn this! ← Advantage of ultra-thin films
Notes: First let me briefly introduce our basic idea.
We plan to use ultrathin ZnO films on metal substrate as model system, and study using LT-SPM.
Ultrathin ZnO films can be prepared in UHV conditions and may be able to control the morphology by the growth conditions.
The structure and property of the ultrathin film is different from the bulk, but they relax to the bulk one rather rapidly with increasing the thickness.
For example, the relaxation to the bulk structure was observed even at 4th of single atomic layers for ZnO on Ag(111).
LT-SPM can provide atomic resolution imaging, local electronic spectroscopy, and local work function measurement.
They will give important insights into the structure, electronic state, and reactivity of HIOS at the single atom/molecule level.
STS is, of course, a very suitable experimental technique to explore this question, then this is an advantage of the use of the conductive ultrathin film.

## Slide 3
Pressure：10-8 Pa
Variable temperature：5 – 300 K
Sample preparation, gas dosing, molecule deposition
Simultaneous measurement of STM/nc-AFM
Laser system
Optics
LT-SPM room
Control unit
Preparation
STM/AFM
Tuning fork sensor
(Omicron GmbH)
F.J. Giessibl, Appl. Phys. Lett. 76, 1471 (2000).
Our instrument – Low-temperature scanning probe microscopy
Bulk ZnO
Notes: I quickly introduce our instruments.
We operate low-temperature scanning probe microscopy.
Using tuning fork sensor, we can measure STM and nc-AFM at the same time.
Laser optics are also quipped in the system, which makes it possible to illuminate the SPM junction in a controlled manner.

## Slide 4
Our instrument – Tip-enhanced Raman spectroscopy (TERS)
C60/Au(111)
Local structural characterization at nm scale!
Strong enhancement of Raman signal under the tip
Illumination of SPM junction causes localized plasmon polariton
Detailed geometrical information
Identification of local defects & molecules
STM image
Raman spectra
Notes: Second, we also have a tip-enhanced Raman spectroscopy in UHV conditions.
Illumination of SPM junction causes localized plasmon plariton, resulting in the strong enhancement of Raman scattering in the vicinity of tip apex.
This is a powerful method to characterize geometrical structure and local defects and molecules.

## Slide 5
STM overview image
Ultrathin ZnO layers grown on Ag(111)
Moiré pattern
Lattice mismatch
between Ag and ZnO
Graphene-like flat structure
(below 3 ML)
Magnified image
About 60 % area is covered by ZnO
Structural model
Atomically-flat and well-defined ZnO layers can be obtained.
Notes: Now I show how the ultrathin ZnO layers look like.
Here shows a Ag(111) surface that is partially covered by ZnO layers.
Here we see only below 3 MLs, which have an atomically-flat graphene-like structure

## Slide 6
C. Tusche, H.L. Meyerheim, J. Kirschner, Phys. Rev. Lett. 99, 026102 (2007).
Structural relaxation of ZnO layers
STM image of thicker ZnO layer
Local defects are visible
Characterization by TERS
Less ordered morphology
(No Moiré pattern)
Detailed geometrical information
Microscopic new insights into the ZnO growth
Relaxation from unusual flat structure to bulk one is revealed by SXRD.
Bridge the discussion between thin film and bulk surface.
Notes: The graphene-like structure is relaxes to bulk (0001) structure at higher layers, which could bridge the discussion between thin films and bulk surface.
As shown here, the thicker layer looks more defective, indicating the transition to the bulk strucutre.
It is very challenging to identify what kind of defects exists.
They will be a good target for the characterization of TERS.

## Slide 7
STM
STS
Local electronic state of ZnO layers
STS spectra for ZnO layers
Local modification of the electronic state can be observed.
Size effect
Edge effect
Local defect
The state shows thickness dependence
Thickness assignment
Notes: Here shows the STS results for ultrathin ZnO layers, and ZnO states are clearly observed with thickness dependence.

## Slide 8
Target molecule
Ladder-type oligo(p-phenylene)s; LOPPs
Synthesized by Hecht group (A3)
Sharp & intense optical transitions
Small Stokes shift
Large extinction coefficient
High fluorescence quantum yield
Currently investigating
L4P-F4
L4P-Sp2
L4P-Sp3

## Slide 9
Preliminary results for LOPPs molecule
Form dimer structure
L4P-sp2 on Au(111)
Herringbone reconstruction
Slightly different adsorption geometry and/or interaction between the molecule and surface
L4P-F4 on Ag(111)

## Slide 10
Overview of our project
Characterize local geometric & electronic structures of molecules & intrinsic defects on ZnO films by LT-SPM
New microscopic insights into the energy level alignment and impact of local defects
Notes: Here is an overview of our project.
We plan to characterize local geometrical & electronic structures of molecules & intrinsic defects in ZnO films using LT-SPM.
I’d like to provide new microscopic insights into the energy level alignment and impact of local defects on that.
To address this fundamental question, I’d like to have a collaborative effort with...

## Slide 11
Overview of our project
I’d like to have a collaboration with
A3(Hecht) for organic molecules
A4(Heimel) for theoretical support
A8(Koch) for comparison of electronic structure at HIOS
B4(Körzendörfer, Scheffler, Rinke) for theoretical support
Notes: Here is an overview of our project.
We plan to characterize local geometrical & electronic structures of molecules & intrinsic defects in ZnO films using LT-SPM.
I’d like to provide new microscopic insights into the energy level alignment and impact of local defects on that.
To address this fundamental question, I’d like to have a collaborative effort with...