## Slide 1
Teilprojekt B3
Sylke Blumstengel, HU Berlin
Electronic coupling in inorganic/organic semiconductor hybrid structures for opto-electronic function

## Slide 2
Results of the first funding period

## Slide 3
Teilprojekt B3 (Blumstengel)
Energy vs. charge transfer in HIOS for light-emitting applications:
ZnO/ZnMgO QW
L4P-Sp3
Energy transfer efficiency:
80 % @ 5 K
32 % @ RT
A3
HIOS unsuited for light-emitting applications!
HIOS:

## Slide 4
Type-II energy level alignment (A8):
Time-resolved PL: hCT ≈ 0.9
Teilprojekt B3 (Blumstengel)
HOMO
LUMO
VBM
CBM
1.5 eV
1.2 eV

## Slide 5
LUMO
HOMO
VBM
CBM
Energy-level tuning by electron-donating interlayer (A5, A8):
Energy transfer efficiency is maintained
Exciton dissociation is suppressed: hCT ≈ 0.45
PL yield is enhanced by a factor of seven
R. Schlesinger, F. Bianchi, S. Blumstengel, C. Christodoulou, R. Ovsyannikov, B. Kobin, K. Moudgil, S. Barlow, S. Hecht, S. R. Marder, F. Henneberger, and N. Koch, submitted.
Energy-transfer cascade:
Teilprojekt B3 (Blumstengel)
LUMO
HOMO
VBM
CBM
Charge transfer
x
LUMO
HOMO
F. Bianchi, S. Sadofev, R. Schlesinger, B. Kobin, S. Hecht, N. Koch, F. Henneberger, and S. Blumstengel, submitted.
Secondary FRET step occurs with efficiency of hET ≈ 1
→ FRET outpaces exciton dissociation
→ Recovery of molecular PL
N. Kedem, S. Blumstengel, F. Henneberger, H. Cohen, G. Hodes and D. Cahen, Phys. Chem. Chem. Phys., 16, 8310 (2014).
FRET
(A3)

## Slide 6
ZnO/organic photovoltaic cells (B7)
ZnO:Ga
ZnO
P3HT
MoO3/Ag
Ag
VOC = 0.304 V, ISC = 0.290 mA/cm², FF = 36.0 %
Teilprojekt B3 (Blumstengel)
-
+
P3HT
ZnO
Next step:
ZnMgO → blueshift of “HCTE” EL
Hybrid charge transfer exciton?

## Slide 7
Goals for second funding period

## Slide 8
Teilprojekt B3 (Blumstengel)
Development of HIOS building blocks for light-emitting devices
FRET in device building blocks studied by optical spectroscopy
Investigation of relevant transfer and injection processes in device building blocks
Proof of principle LED operation
Substrate
molecules
A11 Christiansen
p-GaN
InGaN/GaN or ZnCdO/ZnO
molecules
n-ZnO
S. Blumstengel, H. Kirmse, M. Sparenberg, S. Sadofev, F. Polzer, and F. Henneberger, J. Cryst. Growth 402, 187 (2014).
[00.1]
[01.0]
A5, Z2
Patterning: B13 List-Kratochvil

## Slide 9
Optical excitations at the interface between organic and inorganic semiconductor
Interfacial charge separation and hybrid charge transfer exciton (HCTE) formation
Optical properties of molecules at the semiconductor surface
cw and time-resolved optical spectroscopy, photoreflectivity
→ spectra and dynamics of excitons, HCTE, charged species
EQE and electroluminescence spectra → spectra of HCTE
Differential reflectance spectroscopy → interfacial hybrid exciton formation
Experiments in external magnetic field → recombination pathways of CT exciton
Fokus on epitaxial ZnO or ZnMgO surfaces with different orientation [(0001), (000-1), (10-10), (11-20) ] and modified by molecular monolayers to tune energy levels.
Teilprojekt B3 (Blumstengel)

## Slide 10
Collaborations

## Slide 11
Teilprojekt B3 (Blumstengel)
“Hybrid charge transfer exciton formation”
Complementary experiments: B7 (Neher), B9 (Stähler), A5 (Henneberger), A8 (Koch)
Theory: A4 (Heimel), B6 (May), B11 (Draxl)
Molecules: A3 (Hecht)
“Building blocks for light-emitting devices”
Exchange of materials, fabrication techniques: A11 (Christiansen), B13 (List-Kratochvil)
Energy-level tuning: A8 (Koch)
Exciton dynamics and FRET
Theory: B12 (Knorr/Richter)
Experiment: A6 (Kirstein/Rabe)
Single molecule spectroscopy
B2 (Ballauff, Benson, Lu)