## Slide 1
HIOS PI-Meeting - B2
Coherent amplification and lasing of metal/organic
hybrid structures

## Slide 2
GAIN
surface plasmon lasers
Rodrıguez-Fernandez et al., Langmuir 22, (2006)
CAVITY
Noginov et al., Nature 460, (2009)
Meng et al., NanoLetters (2013)
2009:
CORE-SHELL
2013:
DYE-DOPED
FILM

## Slide 3
Extensive work on synthesis & characterization of spaser architectures
  Hybrid-Core-Shell particles
  Two new setups to investigate single nanoparticles (@HUB: AFM and confocal, @MBI: laser & opt. setup)
Objectives: 1st funding periode
Obj. 1) Synthesis of Spasers
Obj. 2) Investigation of optical properties
Obj. 3) Optimization of gain/loss budget
Standard Spaser design extremely unfeasible
     Aim for better fundamental understanding
    Transition to larger Nanolasers
    Alternative materials
Basic Conclusions
Results

## Slide 4
Obj. 1) synthesis of spasers
Wu et al., Colloid and Polymer Science, (2012)
Synthesis of:
Spherical core-shell particles:
Just like Noginov
& variations
Rod-shaped core-shell particles:
Emitters more in the Red
Layer-by-Layer coated particles
and other approaches

## Slide 5
5/29
Dark-field spectroscopy
AFM imaging
Fluorescence lifetime
Fast fluorescence-pump measurements
Confocal Microscopy
Ti:Sa ~ 488nm
80MHz
Obj. 2) Investigation of opt. prop. @ HU
Problems: fast bleaching, intrinsic gold PL, unknown number of emitters / distances to metal core
Kuhlicke et al., Nano Letters, (2013)
Analytic tools for individual particles
Analytic tools for spaser signatures

## Slide 6
6/29
@ MBI (Ingo Will)
~25ps pulses
527nm
10 Hz
Solving most urgent problems
  Slower bleaching less Gold PL
  reaching inversion
Obj. 2) Investigation of opt. prop. @ MBI
 Inconclusive Laser-Signatures !
Observations:
Random lasing, ASE, Glas PL
Noise to signal transistion can mimic Laser-threshold
Rhodamin
Leaky modes
 Unclear whether standard spaser design works at all !

## Slide 7
7/29
Obj. 3) Optimization of gain/loss budget
Published work: - quasi static approximation (small spheres)
- decay of excited gain medium rendered by single rate
- no competing decay channels
 Explicit incorporation of location- and orientation-dependent decay rates (Busch B10)
SPASER: spacing layer improves performance
 Silicon Nanolaser: silicon competes with silver
Kewes et al., submitted
Kewes et al., in preparation
Kuznetsov et al., Scientific Reports, (2012)

## Slide 8
Conclusions / New Objectives
Accurate spacing and gain layers & well-known dye concentration  synthesis of new systems (Ballauff/Lu B2 and Z2)  Molecular Beam Epitaxy for dye doped films (Blumstengel B3)
Viarbitskaya et al.,
Nature Materials,
(2013)
Better understanding of fundamental processes (few emitters) and competing laser processes, e.g., ASE and random lasing  Theory (Busch B10)  Experiments on a single-to-few emitter level on well defined Gold structures (Benson B2), e.g., with crystalline Gold flakes (Christiansen A11)
Benson, Nature 480, (2011)
Schell et al.,
Rev.Sci.Instr., (2011)
Schell et al.,
Nano Letters,
(2014)

## Slide 9
9/29
Conclusions / New Objectives
Alternative materials: High index dielectrics (e.g. silicon) for resonators  Synthesis of Silicon nanoparticles (Ballauff/Lu B2) and etched Silicon nanowires (Christiansen A11)
 e.g., commerical available polydispersed Si nanoparticles
To get monodisperse particles:
Fractionation by particle size
via centrifugation in a density gradient.
 Surface modification of Silicon nanoparticles
Si
TEOS
H2O, EtOH
pH ~10
SiO2
+
Dye-doped SiO2 with covalent bonding
Route 1:
Route 2:
Si
surface oxidation
Layer-by-layer
Negatively charged-silica surface
PAH-FITC (positive charge)
PSS (negative charge)
Polyelectrolyte chains functionalized with dye molecules
From American Elements company

## Slide 10
10/29
Conclusions / New Objectives
Alternative spaser designs: larger (higher Q-factors), easier to fabricate (e.g. nanowire-cavities / gap plasmon modes)
Gold
Gold-film
Russell et al.,
Nature Photonics,
(2012)
Gold
Dye-doped-film
Gold-film
Kewes et al., APL, (2013)
Numerics for careful designs of efficient gain-to-mode coupling (together with Busch B10)
Chemical synthesis of dye-doped films (Ballauff/Lu B2) and analysis of film thickness (Kirstein A6).

## Slide 11
HIOS PI-Meeting - B2
Coherent amplification and lasing of metal/organic
hybrid structures
Thank you for your attention