## Slide 1
Control of molecular aggregation mode on ZnO surfaces (and other oxides: NiO2,…)
- electrostatic ordering: sexiphenyl and fluorinated sexiphenyl [A3 (Hecht), A9 (Kowarik)]
- symmetry driven: coronene, hexabenzocoronene
- on-surface polymerization: DITF [A3 (Hecht)]
- “service”
New in-situ tools during MBE process
inorganic semiconductor
DRS
B3 (Blumstengel)

## Slide 2
Al2O3/ZnGaO/DITF
0.06 ML
Room temperature STM (n-type ZnO: n ~10 21 cm-3)
0.02 ML
(1010) surface: hexagons, not optimized, STM holder, T < 700 °C
-

## Slide 3
2. n-ZnO as tuneable metal for infrared hybrid plasmonics
- hybridization of surface plasmon polaritons and molecular excitations (vibrational, charge)
[B5 (Wörner, Elsässer)]
- nanostructures for molecular sensing (SEIRA)
C40
proof-of-concept
ATR
Energy (eV)

## Slide 4
Sapphire
dielectric DBR
ZnO/ZnMgO DBR
Hybrid MC
(current design)
L4P
ZnO/ZnMgO MQW
3. Inorganic/organic functional multi-layer structures
- hybrid microcavities (photonic switch, photon and polariton lasing)
- inorganic/organic metamaterials [B10 (Busch)]
cavity dispersion
photon-mediated hybridization of WM and F excitons