## Slide 1: Z2:Monitoring HIOS growth: Surface induced structures and quantitative growth models of anisotropic molecules
Kowarik / Koch

## Slide 2
Surface induced structures
6P
ZnO
ZnO
ZnO
d(100)
AFM
1 µm
HRTEM: 6P on (10-10)ZnO, dE = 10 eV, df = 1000 nm
Surface induced lattice constant 6P-F4 on Zn(000-1)
Critical thickness:
Surface –
bulk structure

## Slide 3
thickness (nm)
25
100
defocus (nm)
-43
50
75
-500
-1000
ZnO
6P
Thickness/defocus map for 6P on (10-10)ZnO
HRTEM simulation
Sabine, Joe?

## Slide 4
BPA
SAM ~6 Å
3FC-BPA
SAM ~10 Å
PFBPA
SAM ~7 Å
Thin
Layer thickness, roughness, density
thin film
θ
θ
q
I. Lange, S. Reiter, M. Pätzel, A. Zykov, A. Nefedov, J. Hildebrandt, S. Hecht, S. Kowarik, C. Wöll, G. Heimel, and D. Neher, Advanced Functional Materials, (2014)).
“Tuning the Work Function of Polar Zinc Oxide Surfaces using Modified Phosphonic Acid Self-Assembled Monolayers”
HIOS morphology: X-ray reflectivity

## Slide 5: Quantitative growth models
"Unravelling the multilayer growth of the fullerene C60 in real-time"
S. Bommel*, N. Kleppmann*, C. Weber, H. Spranger, P. Schäfer, J. Novak, S. V. Roth, F. Schreiber, S. H. L. Klapp, S. Kowarik, accepted (2014) Nature Communications,
Exp.: maximum information, sensitivity, speed
Theory: large systems large timescales

## Slide 6: Growth models for anisotropic molecules
M. Sparenberg*, A. Zykov*, P. Beyer, L. Pithan, C. Weber, Y. Garmshausen, F. Carlà, S. Hecht, S. Blumstengel, F. Henneberger, S. Kowarik, submitted.
Chemical tuning
Rate-equation model for growth

## Slide 7
Non-polar
dipolar
Chemical tuning of morphology
Growth mode, critical cluster size
Atomic Force Microscopy
(Rabe – Kirstein: Do it yourself mode for dummies available)

## Slide 8
Au@Ag Nanorod
Silica shell
2 nm
50 nm
Au
1st SiO2
2nd SiO2 + dye
20 nm
9 nm
HIOS nanostructures: Cryo-TEM
Au-SiO2-PNIPAM
200 nm
Analysis of new systems based on Si-nanoparticles
Notes: Wir haben für B2 alle Systeme und ihre Vorstufen mit CryoTEM und TEM analysiert und brauchen diese Methodik auch für das Fortsetzungsprojekt.

## Slide 9
HIOS nanostructures: Cryo-TEM
J. Mater. Chemistry C, 2014
Semiconductor nanocrystals synthesized on tubular J-aggregates
Notes: Jürgen Rabe kann dazu noch

## Slide 10
In- (experiment & THEORY) | Out-Deliveries
Samples | DIY AFM XRD, XRR (cryo) TEM & SEM images
Growth theory Optimised molecules (dipoles) | in-situ & real-time growth study
Simulation of surface structure | Molecular orientation Exp. Interface structure